Product specification

| Product | CAT5E UTP SOLID 4P | NO. |  | Page | 1/2 |
| --- | --- | --- | --- | --- | --- |
| Edition | 2 | Established Date | 1998-9-23 | Revised Date | 2008/7/23 |
| Approval |  | Checked |  | Finish |  |

Configuration & Physical Characters:

| Conductor | Material | Bare Copper |
| --- | --- | --- |
|  | Construction | 1/0.50 ± 0.01 |
| Insulation | Material | HD-PE |
|  | Thickness | MIN at any point: 0.15mm MAX AVG:0.20 mm |
|  | Diameter | 0.90 ± 0.03 |
|  | Colors | Blue/White-Blue |
|  |  | Orange/White-Orange |
|  |  | Green/White-Green |
|  |  | Brown/White-Brown |
| Jacket | Material | PVC | LSOH | conductor insulation jacket rip cord |
|  | Thickness | MIN at any point: 0.40mm MAX AVG: 0.48mm |  |
|  | Diameter | 5.1 ± 0.3 |  |
|  | Colors | Assorted upon request |  |
|  | Marking | According to production specification |  |

Product specification

| Product | CAT5E UTP SOLID 4P | NO. |  | Page | 2/2 |
| --- | --- | --- | --- | --- | --- |
| Edition | 2 | Established Date | 1998-9-23 | Revised Date | 2006/3/13 |
| Approval |  | Checked |  | Finish |  |

Electric Characters:

| 1. Spark Test | 2000 ± 250 VOC |
| --- | --- |
| 2. Conductor Resistance | MAX 9.50 Ω/100m at 20℃ |
| 3. Resistance Unbalance | MAX 5% |
| 4. Capacitance Unbalance | MAX 330pF/100m |
| 5. Mutual Capacitance | MAX 560pF/100m |
| 6. Impedance | 0.772-100MHz | 100Ω ± 15 |
| Frequency (MHz) | RL (dB) | ATT (dB/100M) at 20℃ | NEXT (Min.dB) | PS-NEXT (Min.dB) |
| 772KHz | 20.0 | 1.8 | 67.0 | 64.0 |
| 1MHz | 20.0 | 2.0 | 65.3 | 62.3 |
| 4MHz | 23.0 | 4.1 | 56.3 | 53.3 |
| 8MHz | 24.5 | 5.8 | 51.8 | 48.8 |
| 10MHz | 25.0 | 6.5 | 50.3 | 47.3 |
| 16MHz | 25.0 | 8.2 | 47.3 | 44.3 |
| 20MHz | 25.0 | 9.3 | 45.8 | 42.8 |
| 25MHz | 24.3 | 10.4 | 44.3 | 41.3 |
| 31.25MHz | 23.3 | 11.7 | 42.9 | 39.9 |
| 62.5MHz | 20.7 | 17.0 | 38.4 | 35.4 |
| 100MHz | 19.1 | 22.0 | 35.3 | 32.3 |